- 产品目录

- Hydroxy Ethylidene-1,1-Diphosphonic Acid (HEDP)

- Amino Trimethylene Phosphonic Acid (ATMP)

- Ethylene Diamine Tetra (Methylene Phosphonic Acid) Sodium (EDTMPS)

- Diethylene Triamine Penta (Methylene Phosphonic Acid) (DTPMPA)

- Hydroxyphosphonocarboxylic Acid (HPAA)

- Phosphonobutane -1,2,4-Tricarboxylic Acid(PBTCA)

- Polyhydric alcohol phosphate ester (PAPE)

- Bis(HexaMethylene Triamine Penta (Methylene Phosphonic Acid)) BHMTPMPA

- Disodium of 1-Hydroxy Ethylidene-1,1-Diphosphonic Acid (HEDP•Na2)

- Tetra sodium of 1-Hydroxy Ethylidene-1,1-Diphosphonic Acid (HEDP•Na4)

- Pentasodium Salt of Ethylene Diamine Tetra (Methylene Phosphonic Acid) (EDTMP•Na5)

- Hepta sodium salt of Diethylene Triamine Penta (Methylene Phosphonic Acid) (DTPMP•Na7)

- Potassium Salt of HexaMethyleneDiamineTetra (MethylenePhosphonic Acid) HMDTMPA•K6

- Polyacrylic Acid  (PAA)

- Polyacrylic Acid Sodium (PAAS)

- Hydrolyzed Polymaleic Anhydride (HPMA)

- Copolymer of Maleic and Acylic Acid (MA/AA)

- Acrylic Acid-2-Acrylamido-2-Methylpropane Sulfonic Acid Copolymer (AA/AMPS)

- Acrylic Acid-2-Hydroxypropyl Acrylate Copolymer (T-225)

- Acrylic Acid/Acrylate/Phosphonic Acid/Sulfosalt Tetra-copolymer (XT-241)

- XT-613 Acrylic-acrylate-sulfosalt copolymers

- Copolymer of Phosphono and carboxylic Acid (PCA)

- XT-1100 Sodium Polyacrylate

- XT-2000 Modified Sodium Polyacrylate

- XT-3100 Carboxylate-Sulfonate-Nonion Tri-polymer

- XT-904 aqueous dispersant

- Polyepoxysuccinic Acid (PESA)

- Dodecyl Dimethyl Benzyl ammonium Chloride (Benzalkonium Chloride,1227)

- Isothiazolinones

- Dodecyl Dimethyl Benzyl ammonium Chloride（Euchlorine）

- XT-402 Composite Bactericide

- XT-406 Composite Bactericide

- XT-409 Sludge Stripper

- XT-503B Scale and Corrosion Inhibitor for Boiler

- XT-504 Scale and Corrosion Inhibitor for Heating Water

- XT-601 Scale and Corrosion Inhibitor for Iron & Steel Plant

- XT-607 Scale Inhibitor for Oilfield Refill Water

- XT-607B Scale Inhibitor for Barium and Strontium

- XT-607B Scale Inhibitor for Barium and Strontium

- XT-619B Scale and Corrosion Inhibitor

- XT-682 Scale and Corrosion Inhibitor for low hardness water

- XT-701 Nonstop Cleaning and Pretreatment Filming Agent

- XT-706 Deoiling Detergent

- XT-707 Pretreatment Filming Agent

- 1,2,3-Benzotrialole (BTA)

- Methylbenzotriazole (TTA)

- Corrosion Inhibitor for Hydrochloric Acid Cleaning

- XT-0100 Antiscalant and Dispersant for RO Membrane

- XT-191 Antiscalant and Dispersant for RO Membrane

- 1-Hydroxy Ethylidene-1,1-Diphosphonic Acid (HEDP)

CAS No. 2809-21-4                                      Dequest:2010

Molecular Formula:   C2H8O7P2                Molecular weight: 206.02

Structural Formula:

- Properties:

HEDP is an organophosphoric acid corrosion inhibitor. It can chelate with Fe, Cu, and Zn ions to form stable chelating compounds.It can dissolve the oxidized materials on these metals’ surfaces. HEDP shows excellent scale and corrosion inhibition effects under temperature 250℃. HEDP has good chemical stability under high pH value, hard to be hydrolyzed, and hard to be decomposed under ordinary light and heat conditions. Its acid/alkali and chlorine oxidation tolerance are better than that of other organophosphoric acids (salt). HEDP can react with metal ions in water system to form hexa-element chelating complex, with calcium ion in particular. Therefore, HEDP has good antiscale and visible threshold effects. When built together with other water treatment chemicals, it shows good synergistic effects.

The solid state of HEDP is crystal powder, suitable for usage in winter and freezing districts. Because of its high purity, it can be used as cleaning agent in electronic fields and as additives in daily chemicals.

- Specification:

| items | index |  |
| --- | --- | --- |
| Appearance | Colorless or light yellow transparent liquid | White crystal powder |
| Active content（HEDP）％ | 58.0-62.0 | 89.0 min |
| Phosphorous acid（as PO33-）% | 2.0 max | 0.5 max |
| Phosphoric acid （asPO43- ）% | 0.8 max | 0.5 max |
| Chloride (as Cl-)% | 0.01 max | 0.01 max |
| pH（1％ solution） | 2 max | 2 max |
| Density （20℃）g/cm3 | 1.40 | — |
| Fe ion ppm | 10 max | 20 max |
| Colour APHA (Hazen) | 40 max | — |

- Usage:

HEDP is used as scale and corrosion inhibition in circulating cool water system, oil field and low-pressure boilers in fields such as electric power, chemical industry, metallurgy, fertilizer, etc.. In light woven industry, HEDP is used as detergent for metal and nonmetal. In dyeing industry, HEDP is used as peroxide stabilizer and dye-fixing agent; In non-cyanide electroplating, HEDP is used as chelating agent. The dosage of 1-10mg/L is preferred as scale inhibitor, 10-50mg/L as corrosion inhibitor, and 1000-2000mg/L as detergent. Usually, HEDP is used together with polycarboxylic acid.

- Package and Storage:

HEDP liquid: Normally In 250kg net Plastic Drum, IBC drum can also be used as required HEDP solid: 25kg inner liner polyethylene (PE) bag, outer plastic woven bag, or confirmed by clients.

Storage for ten months in room shady and dry place.

- Safety Protection:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: HEDP China,Scale inhibitor,1-Hydroxy Ethylidene-1,1-Diphosphonic Acid(HEDP)

Amino Trimethylene Phosphonic Acid (ATMP)

CAS No. 6419-19-8                                                  Dequest: 2000

Molecular Formula:   N(CH2PO3H2)3                 Molecular weight:  299.05

Structural Formula:

- Properties:

ATMP has excellent chelation, low threshold inhibition and lattice distortion ability. It can prevent scale formation, calcium carbonate in particular, in water system. ATMP has good chemical stability and is hard to be hydrolyzed in water system. At high concentration, it has good corrosion inhibition.

ATMP is used in industrial circulating cool water system and oilfield water pipeline in fields of thermal power plant and oil refinery plant. ATMP can decrease scale formation and inhibit corrosion of metal equipment and pipeline. ATMP can be used as chelating agent in woven and dyeing industries and as metal surface treatment agent.

The solid state of ATMP is crystal powder, soluble in water, easily deliquescence, suitable for usage in winter and freezing districts. Because of its high purity, it can be used in woven & dyeing industries and as metal surface treatment agent.

- Specification:

| items | index |  |
| --- | --- | --- |
| Appearance | Colorless or light yellow transparent liquid | White crystal powder |
| Active acid % | 48.0-52.0 | 95 min |
| Chloride (as Cl-)% | 2.0(or1.0) min | 1.0 min |
| pH value（1％ solution） | 2.0 max | 2.0 max |
| Fe (as Fe3+) (ppm) | 20 | 20 |
| Density （20℃）g/cm3 | 1.33 min | — |
| Colour APHA (Hazen) | 40 max | — |

- Usage:

ATMP is usually used together with organophosphoric acid, polycarboxylic acid and salt to built all organic alkaline water treatment agent. ATMP can be used in many different circulating cool water system. The dosage of 1-20mg/L is recommended. As corrosion inhibitor, the dosage of 20-60mg/L is preferred.

- Package and Storage:

ATMP liquid: Normally In 250kg net Plastic Drum, IBC drum can also be used as required ATMP solid: 25kg inner liner polyethylene (PE) bag, outer plastic woven bag, or confirmed by clients.

Storage for ten months in room shady and dry place.

- Safety Protection:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: Amino Trimethylene Phosphonic Acid(ATMP),ATMP China

- Ethylene Diamine Tetra (Methylene Phosphonic Acid) Sodium (EDTMPS)

CAS No. 1429-50-1                                             Dequest: 2040

Molecular Formula:   C6H12O12N2P4Na8          Molecular weight: 612.13

Structural Formula:

- Properties:

EDTMPS is nitrogenous organic polyphosphonic acid, a part of cathodic corrosion inhibitor.Its corrosion inhibition is 3~5 times better than that of inorganic polyphosphate. It can be fully dissolved in water, innocuous and none pollution to environment, has good chemical stability and thermal tolerance. It shows excellent scale inhibition ability under temperature 200℃. It can dissociate into 8 positive-negative ions, thus can chelate with many metal ions to form polymer reticulation complex, to destroy the normal crystallization of calcium scale. EDTMPS shows better antiscale effects to calcium sulfate and barium sulfate.

- Specification:

| items | index |
| --- | --- |
| Appearance | Clear yellow to umber transparent liquid |
| Active component（EDTMPS）％ | 30.0min |
| Organic phosphonic acid（asPO43- ）％ | 10.0min |
| Phosphorous acid（as PO33-）％ | 5.0max |
| Phosphoric acid （asPO43- ）％ | 1.0max |
| pH（1％ water solution） | 9.5-10.5 |
| Density （20℃）g/cm3 | 1.25min |
| Chloride (as Cl-)％ | 3.0max |

- Usage:

EDTMPS can be used as corrosion inhibitor in circulating cool water system and boiler water. It is a chelating agent in non-cyanogen electroplating industry and a water-softening agent in printing & dyeing industry. When used alone, 2~10mg/L is preferred. When built with HPMA by ratio ETDMP:HPMA=1:3, it can be used for low pressure boiler. It can also be built with BTA, PAAS and zinc salt.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

Keywords: Ethylene Diamine Tetra (Methylene Phosphonic Acid) Sodium,EDTMPS,EDTMPS China

Diethylene Triamine Penta (Methylene Phosphonic Acid)
(DTPMPA)

CAS No 15827-60-8                                         Dequest: 2060

Molecular Formula:   C9H28O15N3P5              Molecular weight: 573.2

Structural Formula:

- Properties:

DTPMPA is innocuous, easy to be dissolved in acid solution. DTPMPA has excellent scale and corrosion inhibition and good thermal tolerance ability. DTPMPA can inhibit the scale formation of carbonate, sulfate and phosphate. On situation of alkali environment and high temperature (above 210℃) DTPMPA has better scale and corrosion inhibition effect than other organophosphines.

- Specification:

| items | index |
| --- | --- |
| Appearance | Brown transparent liquid |
| Active acid % | 48.0-52.0 |
| Phosphorous acid（as PO33-）% | 3.0 max |
| Chloride (as Cl-)% | 12-17 |
| Density （20℃）g/cm3 | 1.35-1.45 |
| pH（1％ solution） | 2.0 |
| Fe ppm | 35 max |

- Usage:

DTPMPA can be used as scale and corrosion inhibitor in circulating cool water system and boiler water, and especially in alkali circulating cool water system without additional pH regulation, It can also be used in oilfield refill water, cool water and boiler water with high concentration of barium carbonate. When used alone, little scale sediment is found even none of dispersant is used.

DTPMPA can also be used as peroxide stabilizer, chelating agent in woven & dyeing industry, pigment dispersant, microelement’s carrying agent in fertilizer and concrete modifier. In addition, DTPMPA is used in papermaking, electroplating, acid cleaning and cosmetics.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

- Safety Protection:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: DTPMPA,DTPMPA China,Diethylene Triamine Penta (Methylene Phosphonic Acid)

- 2-Hydroxyphosphonocarboxylic Acid (HPAA)

CAS No 23783-26-8

Molecular Formula:   C2H5O6P                  Molecular weight: 156

Structural Formula:

- Properties:

HPAA is chemically stable, hard to be hydrolyzed, hard to be destroyed by acid or alkali, safety in use, no toxicity, no pollution. HPAA can improve zinc solubility. Its corrosion inhibition ability is 5-8 times better than that of HEDP and EDTMP. When built with low molecular polymers, its corrosion inhibition effect is even better.

- Specification:

| items | index |
| --- | --- |
| Appearance | Dark umber transparent viscous liquid |
| Solid content % | 47.0-50.0 |
| Phosphorous acid（as PO33-）% | 4.0 max |
| Density （20℃）g/cm3 | 1.30 min |
| pH（1％ solution） | 1.0-3.0 |

- Usage:

HPAA is mainly used as cathode corrosion inhibitor in oilfield refill water system in fields such as steel & iron, petrochemcal, power plant and medical industries. When built with zinc salt, the effect is even better.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for one year in room shady and dry place.

Keywords: 2-Hydroxyphosphonocarboxylic Acid(HPAA),HPAA China

- 2-Phosphonobutane -1,2,4-Tricarboxylic Acid(PBTCA)

CAS No. 37971-36-1                               Dequest 7000

Molecular Formula:   C7H11O9P            Molecular weight: 270.13

Structural Formula:

- Properties:

PBTCA has low content of phosphoric, has structural features of both phosphoric acid and carboxylic acid group, which enable its excellent scale and corrosion inhibition properties. Its antiscale property under high temperature is far better than that of organophosphines. It can improve zinc salt solubility, has good chlorine oxidation tolerance and good composite synergy.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow transparent liquid |
| Active acid ％ | 50.0 min |
| Phosphorous acid（as PO33-）% | 0.8 max |
| Phosphorous acid（as PO43-）% | 0.5 max |
| Density （20℃）g/cm3 | 1.27 min |
| pH（1％ solution） | 1.5~2.0 |

- Usage:

PBTCA is a high efficient agent as scale and corrosion inhibitor. It is the excellent stabilizer for zinc salt. It is widely used in circulating cool water system and oilfield refill water system as scale and corrosion inhibitor, suitable to composite with zinc salt and copolymer. It can be used in situations of high temperature, high hardness, high alkali and high concentration index. In lavation fields, it is used as chelating agent and metal detergent.

PBTCA is usually used together with zinc salt, copolymer, organophosphine, imidazole and other Water Treatment Chemicals. When used alone, the dosage of 5-15mg/L is preferred.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for one year in room shady and dry place.

- Safety Protection:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: PBTCA China,2-Phosphonobutane -1,2,4-Tricarboxylic Acid(PBTCA)

Polyhydric alcohol phosphate ester (PAPE)

Structural Formula:

- Properties :

PAPE is a new kind of water treatment chemicals. It has good scale and corrosion inhibition ability. Because more than one ployethylene glycol group is introduced into the molecular, the scale and corrosion inhibition for calcium scale is improved. It has good inhibition effect for barium and strontium scales. PAPE has good scale inhibition effect for calcium carbonate and calcium sulfate, it can mix well with polycarboxylic acid, organophoronic acid, phosphate and zinc salt.

PAPE can be used as scale inhibitor for oilfield (recommended as alternatives of Nalco Visco 953) and industrial cool water system.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow transparent liquid |
| Solid content % | 50.0 min |
| Total phosphoric acid（PO43-）% | 30.0 min |
| Organophosphonic acid（PO43-）% | 15 min |
| pH（1％ solution） | 2.0-3.0 |

- Usage:

when used as scale inhibitor, less than 15mg/L is preferred, when used in closed circulating system, 150mg/L can be expected.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

- Safety Protection:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: Polyhydric alcohol phosphate ester (PAPE),PAPE China

Bis(HexaMethylene Triamine Penta (Methylene Phosphonic Acid)) BHMTPMPA

CAS No. 34690-00-1                                 Dequest: 2090

Molecular Formula: C17H44O15N3P5     Molecular Weight: 685

Structural Formula:

- Properties:

BHMTPMPA is a high-efficient chelating scale inhibitor, it has good effect to carbonate and sulfate scale. BHMTPMPA has good water soluble properties and heat tolerance. BHMTPMPA has high calcium ion tolerance in a wide pH ranges and temperature as high as 120℃.

- Specification:

| items | index |
| --- | --- |
| Appearance | Dark brown liquid |
| Active component % | 43.0-48.0 |
| chloride （Cl-）% | 8.0 max |
| Fe（as Fe3+）ppm | 65 max |
| density（20℃）g/cm3 | 1.23 min |
| PH value (1% water solution) | 2.0 max |

- Usage:

BHMTPMPA can be used as scale and corrosion inhibitor for oilfield water, industrial circulating cool water and boiler.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

- Safety Protection:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: Bis(HexaMethylene Triamine Penta (Methylene Phosphonic Acid)) BHMTPMPA

Disodium of 1-Hydroxy Ethylidene-1,1-Diphosphonic Acid
(HEDP•Na2)

CAS No. 7417-83-7                                  CubleK2012       Dequest: 2016BD

Molecular Formula: C2H6O7P2Na2       Molecular weight: 250

Structural Formula:

- Properties:

HEDP•Na2 is an organophosphonic acid corrosion inhibitor, it can chelate with Fe, Cu, and Zn ions, it can dissolve the oxidized materials, it has good scale and corrosion inhibition effects even under 250℃, it is stable under high pH value, not easy to be hydrolyzed, not easy to be decomposed under normal light and heat condition, its acid/alkaline and chloride oxidation tolerance are better than that of other organophosph-onic acids. HEDP•Na2 can form six-ring chelating compounds with metal ions in water system, Ca2+ in particular. HEDP•Na2 has good scale inhibition effects and obvious dissolution threshold effects. When used with other Water Treatment Chemicals, the synergistic effects is better.

- Specification:

| items | index |  |
| --- | --- | --- |
| Appearance | Colorless to light yellow transparent liquid | White powder |
| Active component（HEDP）％ | 16.5 min | 74.0-79.0 |
| Active component（HEDP•Na2）％ | 20.0 min | 89.8 min |
| density（20℃）g/cm3 | 1.12-1.22 | -- |
| Fe ppm | -- | 35 max |
| Phosphorous acid（PO33-计）% | -- | 3 max |
| Dry weight loss，% | -- | 3-6 |
| PH (1% water solution) | 4.0-6.0 | 4.0-6.0 |

- Usage:

HEDP•Na2 is widely used in circulating cool water system, medium and low pressure boiler, oil field water pipelines as scale and corrosion inhibitor in fields such as electric power, chemical industry, metallurgy, fertilizer, etc.. In light woven industry, HEDP•Na2 is used as detergent for metal and nonmetal. In dyeing industry, HEDP•Na2 is used as peroxide stabilizer and dye-fixing agent; In non-cyanide electroplating, HEDP•Na2 is used as chelating agent.

- Package and Storage:

For liquid: Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

For solid: inner liner polyethylene (PE) bag, outer plastic woven bag, or confirmed by clients. Storage for ten months in room shady and dry place. .

- Safety Protection:

Weak acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: HEDP·Na2 China,Disodium of 1-Hydroxy Ethylidene-1,1-Diphosphonic Acid(HEDP·Na2)

- Tetra sodium of 1-Hydroxy Ethylidene-1,1-Diphosphonic Acid (HEDP•Na4)

CAS No. 29329-71-3 (x-Na), 3794-83-0 (4-Na)     Dequest: 2016/2016DG

Molecular Formula: C2H4O7P2Na4                     Molecular weight: 294

Structural Formula:

- Properties:

Dequest 2016 is the sodium salt of Dequest 2010, HEDP•Na4 is an good scale inhibitor for calcium carbonate, it can be used in low pressure boiler water system, circulating water system, industrial and municipal cleaning water system and swimming pool.

The solid HEDP•Na4 is white powder, soluble in water, easily deliquescence, suitable for use in winter and freezing districts. It is a kind of organophorphonic acid scale and corrosion inhibitor, can form stable complex with Fe, Cu and Zn ions, it can dissolve the oxides on metal surface, it has good scale and corrosion inhibition effect under 250℃.

HEDP•Na4 is widely used in circulating cool water system, medium and low pressure boiler, oil field water pipelines as scale and corrosion inhibitor in fields such as electric power, chemical industry, metallurgy, fertilizer, etc.. In light woven industry, HEDP•Na4 is used as detergent for metal and nonmetal. In dyeing industry, HEDP•Na4 is used as peroxide stabilizer and dye-fixing agent; In non-cyanide electroplating, HEDP•Na4 is used as chelating agent.

- Specification:

| items | index |  |
| --- | --- | --- |
| Appearance | White powder | Colorless to light yellow transparent liquid |
| Active component（HEDP）％ | 56.0 min | 20.3-21.7 |
| Active component（HEDP•Na4）％ | 79.9 min | 29.0-31.0 |
| Total phosphoric acid (as PO43-) ％ | 52.0-54.0 | 18.4-20.4 |
| Fe ppm | 35.0 max | 20 max |
| Dry weight loss，% | 15 max | -- |
| density（20℃）g/cm3 | -- | 1.26-1.36 |
| PH | 11.0-12.0 (1% water solution) | 10.0-12.0 (as it) |

- Package and Storage:

For liquid: Normally In 250kg net Plastic Drum, IBC drum can also be used as required. For solid: inner liner polyethylene (PE) bag, outer plastic woven bag, or confirmed by clients. Storage for ten months in room shady and dry place.

- Safety Protection:

Weak acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: HEDP·Na4 China,Tetra sodium of 1-Hydroxy Ethylidene-1,1-Diphosphonic Acid(HEDP·Na4)

Pentasodium Salt of Ethylene Diamine Tetra (Methylene Phosphonic Acid) (EDTMP•Na5)

CAS No. 7651-99-2                                            Dequest:2006

Molecular Formula: C6H15O12N2P4Na5         Molecular weight: 409

Structural Formula:

- Properties:

EDTMP•Na5 is a neutral solid product. It is nitrogenous organic polyphosphonic acid, which is a part of cathodic corrosion inhibitor. EDTMP•Na5 can be fully dissolved in water, innocuous and none pollution to environment, has good chemical stability and thermal tolerance. EDTMP•Na5 has good scale inhibition property under temperature 200℃. EDTMP•Na5 can dissociate into 8 positive-negative ions, thus can chelate with more than two metal ions to form more than two polymer reticulation complex, the complex can be quickly dissolved in water to destroy the normal crystallization of calcium scale.EDTMP•Na5 shows better scale inhibition effects to calcium sulfate and barium sulfate.

EDTMP•Na5 can be used as scale and corrosion inhibitor for circulating water and boiler water system, chelating agent in non-cyanide electroplating, water-softening agent in dyeing industry, etc.

The solid state EDTMP•Na5 is slightly easy to deliquescence, convenient in transportation and suitable for usage in winter and freezing districts.

- Specification:

| items | index |  |
| --- | --- | --- |
| Appearance | Amber transparent liquid | White powder |
| Active content (EDTMP•5Na)% | 30.0-32.5 | 81.4 min |
| Active content (EDTMPA)% | 24.0-26.0 | 65.0 min |
| Chloride (Cl-) % | 2.0 max | 2.0 max |
| Density (20℃) g/cm3 | 1.25 max | -- |
| Fe（Fe3+）ppm | 20 max | 20 max |
| PH (1% water solution) | 6.0-8.0 | 6.0-8.0 |

- Package and Storage:

For liquid: Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

For solid: inner liner polyethylene (PE) bag, outer plastic woven bag, or confirmed by clients. Storage for one year in room shady and dry place .

Keywords: EDTMP•Na5 China,Pentasodium Salt of Ethylene Diamine Tetra (Methylene Phosphonic Acid) (EDTMP•Na5)

- Hepta sodium salt of Diethylene Triamine Penta (Methylene Phosphonic Acid) (DTPMP•Na7)

CAS No. 22042-96-2 (x-Na) 68155-78-2 (7-Na)       Dequest:2066

Molecular Formula: C9H23O15N3P5Na7                Molecular weight: 727

Structural Formula:

- Properties:

DTPMP•Na7 is a scale inhibitor, for barium sulphate in particular and a chelating agent.DTPMP•Na7 can be used as stabilizer for peroxide bleaching, detergent auxiliaries, in industrial & municipal cleaning water, terrestrial heat water, oilfield water, etc.

- Specification:

| items | index |  |
| --- | --- | --- |
| Appearance | Umber transparent liquid |  |
| Active content (DTPMPA)% > | 31.5-33.5 | 24.0-26.0 |
| Active content (DTPMPANa7)% | 40.0-42.5 | 30.5-33.0 |
| Total phosphoric acid(PO43-)% | 25.9-27.9 | 19.7-21.7 |
| Chloride (Cl-) % | 5.0max | 5.0max |
| Fe ppm | 20max | 20max |
| PH(1% water solution) | 7.0-9.0 | 7.0-9.0 |
| PH(origin solution) | 6.0-8.0 | 6.0-8.0 |
| Density (20℃) g/cm3 | 1.34-1.44 | 1.24-1.34 |

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

- Safety Protection:

Avoid contact with eye and skin, once contacted, flush with water.

Keywords: DTPMP•Na7 China,Hepta Sodium salt of Diethylene Triamine Penta Methylene Phosphonic Acid(DTPMP•Na7)

Potassium Salt of HexaMethyleneDiamineTetra 
(MethylenePhosphonic Acid) HMDTMPA•K6

CAS No. 38820-59-6（X-6） 53473-28-2（6-K）         Dequest 2054

Molecular Formula: C10H22N2O12P4K6         Molecular weight: 721

Structural Formula:

- Properties:

HMDTMPA•K6 is soluble in water, it is a good scale inhibitor for calcium sulfate, suitable for use in situation of high pH value and high alkaline. HMDTMPA•K6 can be used for water treatment in boiler and RO membrane treatment.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless to pale yellow transparent liquid |
| Active component (as acid) ％ | 21.2-24.6 |
| Active component (as salt) ％ | 31.0-36.0 |
| chloride （as Cl-）% | 4.0 max |
| Total phosphoric acid（PO43-）% | 16.8-18.8 |
| Phosphorous acid(as PO33-)，% | 2.0 max |
| Fe ppm | 35 max |
| Density （20℃）g/cm3 | 1.21-1.31 |
| PH (1% water solution) | 6.0-8.0 |

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required.Storage for ten month in room shady and dry place.

Keywords: HMDTMPA•K6 China,Potassium Salt of HexaMethyleneDiamineTetra (MethylenePhosph-onic Acid) HMDTMPA•K6

Polyacrylic Acid  (PAA)

【CAS】 9003-01-4

Structural Formula:

- Properties:

PAA is innoxious and soluble in water, it can be used in situations of alkaline and high concentration without scale sediment. PAA can disperse the microcrystals or microsand of calcium carbonate, calcium phosphate and calcium sulfate. PAA is used as scale inhibitor and dispersant for circulating cool water system, papermaking, weave, dyeing, ceramic, painting, etc.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow transparent liquid |
| Solid content % | 30 min |
| Free monomer (CH2=CH-COOH) % | 0.5 max |
| Density （20℃）g/cm3 | 1.09 min |
| pH（1％ solution） | 3.0 max |

40%, 50% PAA are also supplied.

- Usage:

PAA can be used as scale inhibitor and dispersant in circulating cool water systems in power plants, iron & steel factories, chemical fertilizer plants, refineries and air conditioning systems. Dosage should be in accordance with water quality and equipment materials. When used alone, 1-15mg/L is preferred.

- Package and Storage:

Normally In 200kg net Plastic Drum, IBC drum can also be used as required. Storage for one year in room shady and dry place.

Keywords: PAA China,Polyacrylic Acid(PAA)

Polyacrylic Acid Sodium (PAAS)

【CAS】 9003-04-7

Structural Formula:

- Properties:

PAAS is innoxious and soluble in water, it can be used in situations of alkaline and high concentration without scale sediment. PAAS can disperse the microcrystals or microsand of calcium carbonate, calcium phosphate and calcium sulfate. PAAS is used as scale inhibition and dispersant for circulating cool water system, papermaking, weave, dyeing, ceramic, painting, etc.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow transparent liquid |
| Solid content % | 30 min |
| Free monomer (CH2=CH-COOH) % | 0.5 max |
| Density （20℃）g/cm3 | 1.15 min |
| pH（1％ solution） | 6.0~8.0 |

Notes: Solid content 40%, 45% and 50% are also available

- Usage:

PAAS can be used as scale inhibitor and dispersant in circulating cool water systems in power plants, iron & steel factories, chemical fertilizer plants, refineries and air conditioning systems. Dosage should be in accordance with water quality and equipment materials. When used alone, 2-15mg/L is preferred. When used as dispersant, the dosage should be determined by experiment.

- Package and Storage:

25kg or 200kg in plastic barrel. Storage for ten months in room shady and dry place.

Keywords: PAAS China,Polyacrylic Acid Sodium (PAAS)

Hydrolyzed Polymaleic Anhydride (HPMA)

【CAS】 26099-09-2                           Dequest P9000

Structural Formula:

- Properties:

HPMA is a low molecular weight polymeride, with average molecular weight 400-800. No toxicity, soluble in water, high chemical and thermal stability, decomposed temperature above 330℃. HPMA has obvious threshold effect under high temperature (350℃) and high pH（8.3）level, suitable to be used in alkaline water system or built with agents. It has good scale inhibition against carbonate and phosphate scales under temperature 300℃ with effective time as long as 100 hours. Due to its good scale inhibition and high temperature tolerance properties, HPMA is widely used in desalination plant of flash vaporization equipment, low pressure boiler, steam locomotive, crude oil evaporation, petroleum pipeline, and industrial circulating cool water systems. In addition, HPMA has good corrosion inhibition effect when used together with zinc salt. HPMA can also used as additives for cement.

- Specification:

| items | index |
| --- | --- |
| Appearance | Clear to umber transparent liquid |
| Solid content % | 48.0 min |
| Bromine value mg/g | 80.0 max |
| Average molecular weight | 450 min |
| pH（1％ solution） | 2.0-3.0 |
| Density （20℃）g/cm3 | 1.18 min |

- Usage:

HPMA is usually used together with organic phosphonate at dosage of 1-15ppm for circulating cool water system, oilfield fill water, crude oil dewatering and low-pressure boilers. HPMA has good scale inhibition (98%) and scale stripping properties. When used together with zinc salts, it can effectively inhibit carbon steel corrosion.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required.Storage for one year in room shady and dry place.

- Safety Protection:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: Hydrolyzed Polymaleic Anhydride(HPMA),HPMA China

Copolymer of Maleic and Acylic Acid (MA/AA)

【CAS】 26677-99-6

Structural Formula:

- Properties:

MA/AA is a low molecular weight polyelectrolyte, a copolymer of maleic anhydride and acrylic acid. It has good dispersant performance against carbonate and scale inhibition for phosphate. it has good thermal stability, can be used under high temperature (300℃). MA/AA has good compatibility when used together with other agents. MA/AA is widely used in low-pressure boiler, centralized heating, centralized air-conditioner and circulating cool system. It can also be used as chelating dispersants in woven and dyeing fields.

- Specification:

| items | Water treatment agent | Accessory detergent |
| --- | --- | --- |
| Appearance | Clear brown liquid | amber transparent liquid |
| Solid content % | 48 min | 50 min |
| Free monomer (MA) % | 9.0 max | 5.0 max |
| Density （20℃）g/cm3 | 1.18 min | 1.18min |
| pH（1％ solution） | 2.0~3.0 | 2.0±1.0 |

- Usage:

MA/AA is used in circulating cool water system, medium or lower pressure boiler and distillation system in which high temperature is usually encountered. MA/AA can be used alone or together with other organic phosphates. When used together, the dosage of 2-10mg/L is preferred. The dosage for use as woven & dyeing and accessory detergent should be determined by experiments.

- Package and Storage:

ormally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for one year in room shady and dry place.

- Package and Storage:

Acidity, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: MA-AA China,Copolymer of Maleic and Acylic Acid(MA-AA)

Acrylic Acid-2-Acrylamido-2-Methylpropane Sulfonic Acid Copolymer (AA/AMPS)

【CAS】 40623-75-4

Structural Formula:

- Properties:

AA/AMPS is the copolymer of acrylic acid and 2-acrylanmido-2-methylpropanesulfonic acid (AMPS). Due to including carboxylic group (scale inhibition and dispersion) and sulfonic acid group (strong polarity) in this copolymer, AA/AMPS has high calcium tolerance and good scale inhibition for calcium phosphate, calcium carbonate and zinc scale. When built with organophosphines, the synergic effect is obvious. AA/AMPS is suitable to be used in water quality of high pH and high alkaline, it is one of the ideal scale inhibitor and dispersant on high concentration index.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow viscous liquid |
| Solid content % | 40 min |
| Free monomer （as AA）% | 0.8 max |
| Density （20℃）g/cm3 | 1.15 min |
| pH（1％ solution） | 3.5-4.5 |
| Viscosity mpa.s | 90-200 |

- Usage:

AA/AMPS can be used as scale inhibitor and dispersant in open circulating cool water system, oilfield refill water system, metallurgy system and iron & steel plants to prevent sediment of ferric oxide. When built with organophosphorines and zinc salt, the suitable pH value is 7.0~9.5.

AA/AMPS can also be used as dyeing auxiliaries for textile.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required.Storage for ten months in room shady and dry place.

Keywords: AA-AMPS China,Acrylic Acid-AMPS Copolymer(aa-amps)

Acrylic Acid-2-Hydroxypropyl Acrylate Copolymer (T-225)

【CAS】 55719-33-0

Structural Formula:

- Properties:

T-225 is copolymer of polyacrylic acid and hydroxypropyl acrylate, it has good scale inhibition and dispersion properties to calcium phosphate and calcium carbonate, it has good dispersion properties to ferric oxide sludge, clay and grease. T-225can be used under high pH situation and has good compatibility with other organophosphines and BTA, T-225 can effectively withhold sediments of zinc salt and calcium phosphate, it has good scale inhibition and dispersion properties under high temperature and alkaline situations.

- Specification:

| items | index |  |
| --- | --- | --- |
|  | Neutro | Acid |
| Appearance | Colorless to light yellow viscous liquid |  |
| Solid content % | 30.0 min | 30.0 min |
| Free monomer (as AA )％ | 0.5 max | 0.5 max |
| pH（1％ solution） | 7.5±1.0 | 2.5±0.5 |
| Limiting viscosity number (30℃) dl/g | 0.060～0.095 |  |
| Density （20℃）g/cm3 | 1.10 min |  |

40%, 50% PAA are also supplied.

- Usage:

T-225 can be used in circulating cool water system in situation of alkaline and excess of phosphate. It can be used as scale inhibitor and dispersant for heater, none-column evaporator boiler, circulating cool water and oilfield dirty refilling water with high calcium content. The dosage of 10~30mg/L is preferred. It can be built with organophosphines to form full organic alkaline formula.

- Package and Storage:

Normally In 200kg net Plastic Drum, IBC drum can also be used as required.Storage for one year in room shady and dry place.

Keywords:  Acrylic Acid-2-Hydroxypropyl Acrylate Copolymer T-225

Acrylic Acid/Acrylate/Phosphonic Acid/Sulfosalt 
Tetra-copolymer (XT-241)

- Properties:

XT-241 is copolymer of carboxylic group, hydroxylic group and sulfonic acid group, it has good scale inhibition performance to calcium phosphate and calcium carbonate. XT-241 has good synergic effects with other agents. XT-241is used as scale inhibitor and dispersant in circulating cool water system and built with organophosphate.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow viscous liquid |
| Solid content % | 35.0 min |
| Free monomer （CH2=CH-COOH）% | 0.5 max |
| Density （20℃）g/cm3 | 1.1~1.2 |
| pH（1％ water solution） | 3.0~5.0 |

- Usage:

Normally, the dosage of 5~25mg/L is preferred. When built with organophosphates, the dosage of 1-10mg/L is preferred, the suitable pH value is 7.0-9.5.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. .Storage for one year in room shady and dry place.

Keywords: XT-241 Acrylic Acid/Acrylate/Phosphonic Acid/Sulfosalt Tetra-copolymer

XT-613 Acrylic-acrylate-sulfosalt copolymers

- Properties:

XT-613 is a scale inhibitor and dispersant containing sulfosate and polyelectrolyte. In this copolymer, there exists strong acid, weak acid and non-ion group, it is suitable to be used in high temperature, high pH, high hardness and high alkaline. XT-613 has good scale inhibition for ferric oxide, calcium phosphate, zinc phosphate and calcium carbonate. It has good synergic effect with polyphosphate, zinc salt and other agents.

XT-613 can be used as scale inhibitor and dispersant in industrial circulating water system, oilfield refill water system and boiler water.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow transparent liquid |
| Solid content % | 28.5 min |
| Free monomer （CH2=CH-COOH）% | 1.0 max |
| Density （20℃）g/cm3 | 1.10 min |
| pH（1％ solution） | 4.0-5.0 |

- Usage:

The dosage of 2~40mg/L is preferred depended on water quality and process.

- Package and Storage:

25kg or 200kg in plastic barrel. Storage for ten months in room shady and dry place.

- Safety Protection:

Weak acidity, avoid contact with eye and skin, once contacted, flush with water.

Keywords:  XT-613 Acrylic Acid/Acrylate/Sulfosalt Tri-copolymer

Copolymer of Phosphono and carboxylic Acid (PCA)

- Properties:

Through the introduction of phosphonic group into carboxylic group, PCA has good dispersion property for scale of calcium carbonate and calcium phosphate in circulating cool water system. It has good scale inhibition for barium sulfate, strontium sulfate and silica scale. PCA has advantages in wide range of water quality, chemical stability, strong chlorine tolerance, etc. PCA can be used as scale and corrosion inhibitor in circulating cool water system and oilfield refill water system.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or light yellow liquid |
| Solid content % | 50.0 min |
| Total phosphor （as PO43-）% | 0.5 min |
| Density （20℃）g/cm3 | 1.20-1.30 |
| pH（1％water solution） | 3.0-4.0 |

- Usage:

When used alone, the dosage of 5-20mg/L is preferred. It can also be used together with organophosphines, copolymer, zinc salt or BTA.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required.Storage for ten months in room shady and dry place.

Keywords: PCA China,Copolymer of Phosphono and carboxylic Acid (PCA)

XT-1100 Sodium Polyacrylate

Structural Formula:

- Properties:

XT-1100 is the homopolymer of low molecular polyacrylic acid and its salts. Free of phosphate, it can be used in situations of low or none content of phosphate. XT-1100 can be used as high effective scale inhibitor for sugar processing. XT-1100 obtains the scale inhibition effect by dispersing calcium carbonate or calcium sulfate in water system. XT-1100 is an ordinary used dispersant, it can be used as scale inhibitor and dispersant in circulating cool water system, papermaking, woven and dyeing, ceramics and pigments. (similiar to RohmHaas Co. ACUMER 1100)

- Specification:

| items | index |
| --- | --- |
| Appearance | Light amber liquid |
| Solid content % | 47.0-49.0 |
| Density （20℃）g/cm3 | 1.22 min |
| pH（1％water solution） | 3.2-4.0 |

- Usage:

When used alone, the dosage of 10-30mg/L is preferred. When used as dispersant in other fields, the dosage should be determined by experiment.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

Keywords: Sodium Polyacrylate

- XT-2000 Modified Sodium Polyacrylate

- Properties:

XT-2000 is the copolymer of acrylic-acrylate-sulfosate, it is a good scale inhibitor for calcium phosphate, calcium carbonate and other inorganic minerals. XT-2000 can effectively stabilize calcium phosphate in formula containing phosphate. It can also stabilize zinc in formula containing zinc. It can disperse inorganic microparticles without pH influence.

XT-2000 is an effective dispersant in all organic water treatment formula, it can be used as dispersant for minerals, stabilizer for calcium phosphate. (similiar to RohmHaas Co. ACUMER 2000)

- Specification:

| items | index |
| --- | --- |
| Appearance | Light amber liquid |
| Solid content % | 42.5-43.5 |
| Density （20℃）g/cm3 | 1.21 min |
| pH（1％water solution） | 3.8 - 4.6 |

- Usage:

XT-2000 can be used as scale inhibitor for circulating cool water and boiler water, for phosphate, zinc ion and inorganic minerals in particular. When used alone, the dosage of 10-30mg/L is preferred. When used in other fields, the dosage should be determined by experiment.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

Keywords: Modified Sodium Polyacrylate

XT-3100 Carboxylate-Sulfonate-Nonion Tri-polymer

- Properties:

XT-3100 is a good scale inhibitor and dispersant for cool water treatment, it has good inhibition for dry or hydrated ferric oxide. XT-3100 is a all organic dispersant and scale inhibitor, it can be also used as stabilizer of corrosion inhibitor for phosphate and phosphinic salt. (Similiar to RohmHaas ACUMER 3100)

- Specification:

| items | index |
| --- | --- |
| Appearance | Light amber liquid |
| Solid content % | 43.0-44.0 |
| Density （20℃）g/cm3 | 1.20 min |
| pH（1％water solution） | 2.1-2.6 |

- Usage:

XT-3100 can be used as scale inhibitor for circulating cool water and boiler water, for phosphate, zinc ion and ferric in particular. When used alone, the dosage of 10-30mg/L is preferred. When used in other fields, the dosage should be determined by experiment.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required.Storage for ten months in room shady and dry place.

Keywords: Carboxylate-Sulfonate-Nonion Tri-polymer

- XT-904 aqueous dispersant

Alias: Viscosity Reduer, Water Reducer, Grind Aider

- Properties:

The main composition of dispersant XT-904 is anion polymer. It can adsorb on surface of microparticles resulting in static repulsion, resulting in disperse and preventing sedimentation and coarse turn-back. XT-904 is little foaming, innocuous, non-corrosiveness and non-hazardous.

XT-904 is used as chelant in papermaking coating, building coating, concrete retarder, water reducer, woven and dyeing. Its performance can reach to that of SN-5040. Adding XT-904 to slurry during grinding process of bolus alba, lime carbonate, pottery clay, titanium pigment, French chalk, barium sulfate, coal-water slurry, etc., the viscosity can be largely reduced and the dispersed slurry is stable.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless to light yellow viscous liquid |
| Solid content % | 40.0 min |
| pH value (2% water solution) | 8.0~11.0 |
| Density （20℃）g/cm3 | 1.20 min |
| Viscosity（25℃）mpa.s | 200—600 |

- Usage:

The dosage of 0.2-2% is preferred (solid/solid), the optimal dosage should be determined by experiment.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

Keywords:  aqueous dispersant,viscosity reducing agent, water reducing agent, grinding aid agent

Polyepoxysuccinic Acid (PESA)

Molecular Formula:   HO(C4H2O5M2)nH                 Molecular weight:  400-1500

Structural Formula:

- Properties:

PESA is a multivariate scale and corrosion inhibitor with non-phosphor and non-nitrogen, it has good scale inhibition and dispersion for calcium carbonate, calcium sulfate, calcium fluoride and silica scale, with effects better than that of ordinary organophosphines. When built with organophosphates, the synergism effects are obvious.

PESA has good biodegradation properties, it can be widely used in circulating cool water system in situation of high alkaline, high hardness and high pH value. PESA can be operated under high concentration index. PESA has good synergism with chlorine and other Water Treatment Chemicals.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless or amble transparent liquid |
| Solid content % | 40.0 min |
| Density （20℃）g/cm3 | 1.28 min |
| pH（1％water solution） | 9.0-12.0 |

- Usage:

PESA can be used in system of oilfield refill water, crude oil dehydration and boiler; PESA can be used in circulating cool water system of steel, petrochemical, power plant, medicine.

PESA can be used in boiler water, circulating cool water, desalination plant, and membrane separation in situation of high alkaline, high hardness, high pH value and high concentration index. PESA can be used in detergent fields.

- Package and Storage:

Normally In 250kg net Plastic Drum, IBC drum can also be used as required. Storage for ten months in room shady and dry place.

- Safety Protection:

Alkaline, Avoid contact with eye and skin, once contacted, flush with water.

Keywords: PESA China,polyepoxysuccinic Acid (PESA)

Dodecyl Dimethyl Benzyl ammonium Chloride
(Benzalkonium Chloride,1227)

CAS No.  8001-54-5 or 63449-41-2, 139-07-1        Molecular weight:  340.0

Molecular Formula:  C21H38NCl

Structural Formula:

- Properties:

Benzalkonium Chloride is a kind of cationic surfactant, belonging to nonoxidizing boicide. It can efficiently withhold algae propagation and sludge reproduction. Benzalkonium Chloride also has dispersing and penetrating properties, can penetrate and remove sludge and algae, has advantages of low toxicity, no toxicity accumulation, soluble in water, convenient in use, unaffected by water hardness. Benzalkonium Chloride can be also used as anti-mildew agent, antistatic agent, emulsifying agent and amendment agent in woven and dyeing fields.

- Specification:

| items | index |  |  |
| --- | --- | --- | --- |
| Appearance | colorless to pale yellow transparent liquid | light yellow transparent liquid | light yellow waxy solid |
| Solid content ％ | 44.0 min | 80 min | 88 min |
| Amine salt ％ | 2.0 max | 2.0 max | 2.0 max |
| pH（1% water solution） | 6.0~8.0（origin） | 6.0-8.0 | 6.0-8.0 |
|  | normal | good fluid | bad fluid |

- Usage:

As nonoxidizing boicide, dosage of 50-100mg/L is preferred; as sludge remover, 200-300mg/L is preferred, adequate organosilyl antifoaming agent should be added for this purpose. This product can be used together with other fungicidal such as isothiazolinones, glutaraldegyde, dithionitrile methane for synergism, but cannot be used together with chlorophenols. If sewage is appeared after thrown of this product in circulating cool water, the sewage should be filtered or blown off in time to prevent their deposit in bottom of collecting tank after froth disappearance.

No blending with anion surfactant.

- Package and Storage:

25kg or 200kg in plastic barrel, or confirmed by clients. Storage for two year in room shady and dry place.

- Safety Protection:

A little smell of almond, no visible stimulation to skin. When contacted, flush with water.

Keywords: Dodecyl Dimethyl Benzyl ammonium Chloride 1227

- Isothiazolinones

【CAS】 26172-55-4, 2682-20-4            Molecular weight:  115.16

Structural Formula:

2-methyl-4-thiazoline-3-ketone         5-chloro- methyl-4-thiazoline-3-ketone

- Properties:

Isothiazolinones is composed of 5-chloro-2-methyl-4-thiazoline-3-ketone (CMI) and 2-methyl-4-thiazoline-3-ketone (MI). The bactericidal effect of Isothiazolinones is carried out through breaking the bond between bacteria and algae protein. When contacted with microbes, Isothiazolinones can quickly inhibit their growth, thus leading to death of these microbes. Isothiazolinones has strong inhibition and biocidal effects on ordinary bacteria, fungi and alga, and has many advantages such as high biocidal efficiency, good degradation, no residual, safety in operation, good compatibleness, good stabilization, low cost in operation.

Isothiazolinones can mix with chlorine and most cation, anion, and non-ionic surfactants. When used at high dosage, its biosludge stripping effect is excellent.

Isothiazolinones is a kind of fungicidal with properties of broad spectrum, high efficiency, low toxicity and non-oxidative, it is the ideal biocidal in industrial circulating cool water system and in wastewater treatment in oilfield, papermaking, pesticide, cutting oil, leather, detergent and cosmetics etc..

- Specification:

Notes: 2%, 4% and 8% or any concentration can be supplied on demands.

| items | index |  |
| --- | --- | --- |
|  | Grade I | Grade II |
| Appearance | Amber transparent liquid | Light yellow or light green transparent liquid |
| Active content ％ | 14.0 min | 1.50 min |
| pH value（as it） | 1.0-4.0 | 2.0-5.0 |
| Density （20℃）g/cm3 | 1.25 min | 1.02 min |
| CMI/MI (wt %) | 2.5-4.0 | 2.5-4.0 |

- Usage:

When used as sludge stripper for grade II, the dosage of 150-300mg/L is preferred, when used as boicide, the dosage of 80-100mg/L is preferred, and charges every 3-7 days. No used together with oxidative fungicidal such as chlorine, and no used in cooling water system containing sulfur. When used together with quaternary amine, the effect will be better. When used as industrial fungicide, the dosage of 0.05-0.4% is preferred.

- Package and Storage:

25kg in plastic barrel, or confirmed by clients. Storage for ten months in room shady and dry place.

- Safety Protection:

Corrosive, Avoid contact with eye and skin, Wear splash resistant safety goggles and rubber glores.once contacted, flush with water.

Keywords: Isothiazolinones,Isothiazolinones China

- Dodecyl Dimethyl Benzyl ammonium Chloride
（Euchlorine）

- Properties:

Euchlorine is water soluble, it has properties of high effective, instant effective, wide range and safety. Euchlorine has strong fungicide effect, even at dosage of 20ppm, the fungicide ratio can reach to 99%. Euchlorine has good stability, can be preserved for half year with less than 1% loss of effective chlorine, and cannot be deteriorated at 120℃, cannot be flamed.

- Usage:

Euchlorine can be used as algae disinfector in circulating cool water system and swimming pool. When used in circulating cool water system, the dosage of 15-20ppm every 2-3 days in Summer is preferred, in Spring and Autumn, every 3-5 days and in Winter every 5-7 days. For insurance of effects, nonoxidative disinfector may be also added into this product.

- Package and Storage:

25kg inner liner polyethylene (PE) bag, outer plastic woven bag, or determined by clients. Storage for one year in room shady and dry place.

- Safety Protection:

Stimulation to skin and eye, protected with eye-glass and glove in operation. Once contacted, flush with water.

Keywords: Dodecyl Dimethyl Benzyl ammonium Chloride（Euchlorine）

- XT-402 Composite Bactericide

- Properties:

XT-402 is composed of quaternary ammonium salt and isothiazolinone. XT-402 has the advantages of high efficiency, wide range, low toxicity, quick effect and durable, strong penetration, convenience in use, and wide range of suitable temperature and pH, no drug resistance even after long period of using.

- Specification:

| items | index |
| --- | --- |
| Appearance | Yellow greenish transparent liquid |
| pH（1% water solution） | 2.5-4.5 |
| Density （20℃）g/cm3 | 1.0±0.05 |

- Usage:

XT-402 can be used as fungi disinfectant and sludge stripper in industrial circulating cool water systems in fields such as power plant, chemical industry, fertilizer, oil refining and metallurgy. Its effect is better that that of 1227. In addition, this product has certain effect of corrosion inhibition.

Impact charge, dosage of 80-200mg/L will kill all algae. Enlarge dosage if wish to quickly remove multitude algae. Clean out the removed sludge and floatages to prevent their deposit. Once existed more foams, antifoaming agent should be added. NO blend with anion surfactant.

- Package and Storage:

25kg in plastic barrel, or confirmed by clients. Storage for six months.

- Safety Protection:

Stimulation to skin, once contacted, flush with water.

Keywords: XT-402 Composite Bactericide

XT-406 Composite Bactericide

- Properties:

XT-406 is a kind of fungi disinfectant composed of quaternary ammonium salt. XT-406 has the advantages of high efficiency, low toxicity, quick effect and durable, strong penetration, convenience in use, and wide ranges of suitable temperature and pH.

XT-406 can be used as fungi disinfectant and sludge stripper in industrial circulating cool water systems in power plant, chemical industry, fertilizer, oil refining and metallurgy. Its effect is better that that of 1227.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless transparent liquid |
| Active content，％ | 30.0min |
| Amine salt ％ | 2.0 max |
| pH (as it) | 6.0-8.0 |

- Usage:

Impact charge, dosage of 80-100mg/L will kill all algae. Enlarge dosage if wish to quickly remove multitude algae. Clean out the removed sludge and floatage to prevent their deposit. Once existed more foams, antifoaming agent should be added.

- Package and Storage:

25kg in plastic barrel, or confirmed by clients. Storage for one year.

- Safety Protection:

A little smell of almond, no visible stimulation to skin. When contacted, flush with water.

Keywords: XT-406 Composite Bactericide

- XT-409 Sludge Stripper

- Properties:

XT-409 is composed of cationic surfactant, penetrating agent and dispersant. XT-409 has the advantages of high efficiency, wide range, sterilization, fungicidal, sludge stripping and cleaning. XT-409 has good disperse and penetration properties, low toxicity, fast effective, it has good sludge stripping effect for sludge, plastocene, bacteria secretion, and fungus. XT-409 can soften and clean the scale on metal surface. XT-409 is not corrosive to metal, rubble and plastics, soluble in water, not affected by water hardness. XT-409 is used as sludge stripper in circulating water system, it can also used as algae disinfector, cleaning agent and papemaking anticorrosive.

- Specification:

| items | index |
| --- | --- |
| Appearance | Colorless, light muddy liquid |
| Active content，％ | 30.0 min |
| pH | 6.0-8.0 |

- Usage:

The dosage of 100-200ppm is preferred according to water content. Enlarge dosage if wish to quickly remove multitude algae. Clean out the removed sludge and floatage to prevent their deposit. When used as fungicidal, 50-100ppm is preferred. No blend with anion surfactant and no blend with chlorophenol agents.

- Package and Storage:

25kg or 200kg in plastic barrel, or confirmed by clients. Storage for one year in room shady and dry place.

- Safety Protection:

No visible stimulation to skin. When contacted, flush with water.

Keywords: Sludge Stripper

XT-503B Scale and Corrosion Inhibitor for Boiler

- Properties and Usage:

XT-503B is composed of chelating, cleaning and dispersing agents. XT-503B has effects of both cleaning and corrosion inhibition, and has the advantages of fast cleaning, good effect, low corrosion rate.XT-503B has little damage to boiler body and is not affected by Fe and Cu ions in water system, it is suitable for medium/low pressure boiler.

- Specification:

| items | index |
| --- | --- |
| Appearance | Amber liquid |
| Solid content， % | 40.0 min |
| Density，（20℃）g/cm3 | 1.25±0.1 |
| pH，（1% water solution） | 2.0±1.0 |

- Usage:

The dosage of 1-3‰ is preferred according to boiler body volume and scale quantity.

- Package and Storage:

25kg in plastic barrel. Storage in room shady and dry place for one year.

Keywords: Scale and Corrosion Inhibitor for Boiler

XT-504 Scale and Corrosion Inhibitor for Heating Water

- Properties:

XT-504 is mainly composed of high efficient chelating agent. Through reaction between chelating agent and metal surface, a protective film is formed. XT-504 has crystal distortion effect on calcium carbonate and calcium sulfate, thus the formed scale cannot firmly absorb on vessel wall. This product has the advantages of high temperature tolerance, high scale inhibition effect, hard to decomposed, free of carcinogenic substance such as sodium nitrite, full organic composite, good bio-degradation property. XT-504 is a kind of environmental greenish scale and corrosion inhibitor for heating water.

XT-504 can be directly used as scale and corrosion inhibitor for heating water. Because the process of softening is omitted, the cost for heating is largely decreased, great economic and social profits to enterprises may be expected.

- Usage:

According to water quality, 50-200g per ton water is preferred to the heating water system. If the make-up water is in midway, add quantity in proportion.

- Package and Storage:

25kg in plastic barrel, or confirmed by clients. Storage for one year in room shady and dry place.

- Safety Protection:

Nontoxic, once contact skin, flush with water.

Keywords: Scale and Corrosion Inhibitor

- XT-601 Scale and Corrosion Inhibitor for Iron & Steel Plant

- Properties:

XT-601 is built with organophosphoric acid, polycarboxylic acid and carbon iron corrosion inhibitor, it can effectively chelate and disperse calcium carbonate and calcium phosphate scales. XT-601 has good scale inhibition effect on steel & iron in open wide circulating cool water system. It has the advantages of effective and strong corrosion inhibition.

- Specification:

| items | index |
| --- | --- |
| Appearance | Amber liquid |
| Solid content，% | 30.0 min |
| Total phosphoric acid，（as PO43-）% | 15.0 min |
| pH，（1%water solution） | 2.0±1.0 |
| Density（20℃） , g/cm3 | 1.10 |

- Usage:

Add XT-601 into plastic pool (or box) every day, dilute with water and continuously add into inlet of dosage pump or metering valve (outlet of collecting tank). Dosage of 5-20mg/L is preferred (according to quantity of makeup water).

- Package and Storage:

25kg or 200kg in plastic barrel, or confirmed by clients. Storage for ten months in room shady and dry place.

Keywords: Scale and Corrosion Inhibitor for Iron & Steel Plantn

- XT-607 Scale Inhibitor for Oilfield Refill Water

- Properties:

XT-607 is built with organophosphoric acid, special surfactant and synergistic agents, It can chelate with Ca2+ and Mg2+. XT-607 can effectively chelate and disperse calcium carbonate, calcium sulfate and calcium phosphate scales. XT-607 is used as scale inhibitor for pipeline of oilfield refill water. It has the advantages of high temperature tolerance, alkaline tolerance, salt tolerance, stable in oilfield reservoir, low dosage, etc.

- Specification:

| items | index |
| --- | --- |
| Appearance | colorless or light yellow liquid |
| Solid content，% | 30.0 min |
| pH，（1%water solution） | 2.0±1.5 |
| Density（20℃）, g/cm3 | 1.10 min |

- Usage:

Add XT-607 into plastic pool (or box) every day, dilute with water and continuously add into inlet of dosage pump or metering valve (outlet of collecting tank). Dosage of 10-50ppm is preferred (according to quantity of makeup water).

- Package and Storage:

25kg or 200kg in plastic barrel, or confirmed by clients. Storage for ten months in room shady and dry place.

Keywords: Scale Inhibitor for Oilfield Refill Water

XT-607B Scale Inhibitor for Barium and Strontium

- Properties:

XT-607B is designed for stabilizing of Ba2+ and Sr2+. XT-607B can effectively stabilize Ba2+ and Sr2+ in water system. XT-607B has good scale inhibition effect for calcium carbonate, calcium sulfate, and magnesium sulfate, it can be used in oilfield refill water system and industrial circulating cool system.

- Specification:

| items | index |
| --- | --- |
| Appearance | Amber transparent liquid |
| Solid content，% | 40.0 min |
| pH，（1%water solution） | 6.0 min |
| Density（20℃）, g/cm3 | 1.10 min |

- Usage:

Add XT-607B into plastic pool (or box) every day, dilute with water and continuously add into inlet of dosage pump or metering valve (outlet of collecting tank). Dosage of 10-50ppm is preferred (according to quantity of makeup water).

- Package and Storage:

25kg or 200kg in plastic barrel, or confirmed by clients. Storage for ten months in room shady and dry place.

Keywords: Scale Inhibitor for Barium and Strontium,Scale Inhibitor

XT-607B Scale Inhibitor for Barium and Strontium

- Properties:

XT-607B is designed for stabilizing of Ba2+ and Sr2+. XT-607B can effectively stabilize Ba2+ and Sr2+ in water system. XT-607B has good scale inhibition effect for calcium carbonate, calcium sulfate, and magnesium sulfate, it can be used in oilfield refill water system and industrial circulating cool system.

- Specification:

| items | index |
| --- | --- |
| Appearance | Amber transparent liquid |
| Solid content，% | 40.0 min |
| pH，（1%water solution） | 6.0 min |
| Density（20℃）, g/cm3 | 1.10 min |

- Usage:

Add XT-607B into plastic pool (or box) every day, dilute with water and continuously add into inlet of dosage pump or metering valve (outlet of collecting tank). Dosage of 10-50ppm is preferred (according to quantity of makeup water).

- Package and Storage:

25kg or 200kg in plastic barrel, or confirmed by clients. Storage for ten months in room shady and dry place.

Keywords: Scale Inhibitor for Barium and Strontium,Scale Inhibitor

- XT-619B Scale and Corrosion Inhibitor

- Properties:

XT-619B is composed of organophosphoric acid, polycarboxylic acid, sulfosalt copolym-ers, copper corrosion inhibitor, special surfactant, etc. The organophosphine acid forms protection membrane and brings corrosion inhibition on metal surface. XT-619B has good chelation and lattice distortion effect on calcium carbonate, calcium sulfate and calcium phosphate. Through rational prescription, XT-619B has good synergistic effect, with high corrosion inhibition ratio, high temperature tolerance, high scale inhibition ratio and not easy to degradation.

- Specification:

| items | index |
| --- | --- |
| Appearance | Amber transparent liquid |
| Solid content，% | 30.0 min |
| Total phosphoric acid，（as PO43-）% | 8.0 min |
| pH，（1%water solution） | 2.0±1.0 |
| Density（20℃） , g/cm3 | 1.10 min |
| Thiazole (as C6H5N3) | 1.5 min |

- Usage:

Add XT-619B into plastic pool (or box) every day, dilute with water and continuously add into inlet of dosage pump or metering valve (outlet of collecting tank). The dosage of 5-30ppm is preferred.

- Package and Storage:

25kg or 200kg in plastic barrel, or confirmed by clients. Storage for one year in room shady and dry place.

Keywords: Scale and Corrosion Inhibitor

- XT-682 Scale and Corrosion Inhibitor for low hardness water

- Properties:

XT-682 is built with surfactant, dispersant, corrosion inhibitor, etc. It is suitable for system using soften water and other low hardness water as cool media. Because there are little contents of Ca2+ and Mg2+ ions in soften water, scale cannot be formed. Many corrosion inhibitors use Ca2+ and Mg2+ ions in water system to form protection membrane on metal surface, but there are little contents of Ca2+ and Mg2+ ions in soften water, the corrosion inhibition is a difficult question for soften water system. Through experiments, we develop this greenish scale and corrosion inhibitor for soften water system. XT-682 is a composite corrosion inhibitor by inhibition of metal polarization. XT-682 has no contents of such noxious subjects as nitrite and chromate, no pollution to environment, its corrosion ratio to carbon steel far lower than that of national standard.

- Specification:

| items | index |
| --- | --- |
| Appearance | yellow transparent liquid |
| Solid content，% | 30.0 min |
| pH，（1%water solution） | 3.0±1.5 |
| Density（20℃） , g/cm3 | 1.20 min |

- Usage:

Add XT-682 into plastic pool (or box) every day, dilute with water and continuously add into inlet of dosage pump or metering valve (outlet of collecting tank). The dosage of 30-70ppm is preferred.

- Package and Storage:

25kg in plastic barrel, or confirmed by clients. Storage for ten months in room shady and dry place.

Keywords: Scale and Corrosion Inhibitor

XT-701 Nonstop Cleaning and Pretreatment Filming Agent

- Properties:

XT-701 is composed of chelating, detergent, dispersant and pretreatment filming agent. It has properties of fast cleaning, quick filming, film homogeneization, and low corrosion ratio. It is not affected by ferric and copper ions in pretreatment filming, especially suitable to be used in nonstop cleaning of circulating water system.

- Specification:

| items | index |
| --- | --- |
| Appearance | Amber liquid |
| Solid content，% | 40.0 min |
| Total phosphoric acid acid (asPO43-) % | 20.0 min |
| Density（20℃） , g/cm3 | 1.25±0.1 |
| pH，（1%water solution） | 2.0±1.0 |

- Usage:

The dosage of 150-250mg/L is preferred.

- Package and Storage:

25kg barrel or confirmed by clients. Storage for one year in room shady and dry place.

Keywords: Nonstop Cleaning and Pretreatment Filming Agent,Filming Agent

- XT-706 Deoiling Detergent

- Properties:

XT-706 is composed of chelating, cleaning, deoiling, dispersant and penetrating agent. It is a good deoiling detergent with properties of deoiling, descaling and cleaning. XT-706 can effectively remove the scale, oil film and emulsified oil. XT-706 is compatible with phosphorus series scale and corrosion inhibitors.

- Specification:

| items | index |
| --- | --- |
| Appearance | Brown turbid liquid |
| Solid content，% | 30.0 min |
| Density（20℃） , g/cm3 | 1.25±0.1 |
| pH，（1%water solution） | 2.0±1.0 |

- Usage:

The dosage is determined by the actual circulating cool water system, ask the engineer for detail.

- Package and Storage:

25kg barrel or confirmed by clients. Storage for six months in room shady and dry place.

- Safety Protection:

Acidity, avoid contact with eye and skin, once contacted, flush with water.

Keywords: Deoiling Detergent

- XT-707 Pretreatment Filming Agent

- Properties:

XT-707 is composed of chelating agent, dispersant, pretreatment filming and surfactant. The chelating agent can chemically adsorb ferric and calcium, forming a hard film on metal surface. It has the advantages of quick filming, film homogeneization, chemical stable and low corrosion ratio. It can be used as pretreatment filming agent for equipment and pipeline of new system or after heavy repair. XT-707 is not affected by copper and ferric ions in water system.

- Specification:

| items | index |
| --- | --- |
| Appearance | Amber transparent liquid |
| Solid content，% | 40.0 min |
| Density（20℃） , g/cm3 | 1.25±0.1 |
| pH，（1%water solution） | 2.0±1.0 |

- Usage:

The dosage of 200-500mg/L is preferred. Pretreatment filming time for cold state is 48-72 hours, and for heat state is 24-48 hours.

- Package and Storage:

25kg barrel or confirmed by clients. Storage for one year in room shady and dry place.

- Safety Protection:

Acidity, avoid contact with eye and skin, once contacted, flush with water.

Keywords: Pretreatment Filming Agent,Filming Agent

1,2,3-Benzotrialole (BTA)

- CAS No 95-14-7

- Specification:

| items | index |
| --- | --- |
| Appearance | Yellow transparent liquid |
| Active content(wt) % | 30.0 min |
| Density（20℃） , g/cm3 | 1.12±0.1 |

- Properties and Usage:

This product can be absorbed on metal surface and form a thin film to protect copper and other metals. It can be used together with many scale inhibitors and fungi disinfectants in circulating cool water system, it has good corrosion inhibition effect in circulating cool water system. The dosage of 2-4mg/L is preferred. This product can also be used as anti-discolor agent, coating additives and luboil additive.

- Package and Storage:

25kg in plastic barrel, or confirmed by clients. Storage for six months in room shady and dry place.

Keywords: BTA China,1,2,3-Benzotrialole(BTA)

- 2-Mercaptobenzothiazole (MBT)

- CAS No 149-30-30

- Specification:

| items | index |
| --- | --- |
| Appearance | Yellow transparent liquid |
| Active content(wt) % | 50.0 min |
| Density（20℃） , g/cm3 | 1.20 min |

- Properties and Usage:

This product can be used as the copper corrosion inhibitor in circulating cool water system. The mechanism is due to the chemical absorption of MBT on copper surface, or chelation reaction between them. The dosage of 4mg/L is preferred. This product can also be used as plasticizer and photometer for acid copper plating.

- Package and Storage:

25kg in plastic barrel, or confirmed by clients. Storage for six months in room shady and dry place.

Keywords: MBT China,2-Mercaptobenzothiazole(MBT)

- Methylbenzotriazole (TTA)

- CAS No 29385-43-1

- Molecular formula: C7H7N3       Molecular Weight: 133.16

- Specification:

| items | index |
| --- | --- |
| Appearance | White or Light yellow particle shape solid |
| Active contentwt % | 99.0 min |
| Melting point ℃ | 80-86 |
| Ash content % | 0.1 max |
| Water content % | 0.2 max |

- Properties:

TTA can be used as corrosion inhibitor of copper and copper alloy, it also has corrosion inhibition for black metals. This product is absorbed on metal surface to form a thin membrane to protect copper and other metals from corrosion of air and other harmful subjects. The membrane is more uniform. When used together with MBT, the effect is better.

- Usage:

First, dissolved with alcohol or alkali, then added into circulating water system, the dosage of 2-10mg/L is preferred. If the metal is badly corroded, 5-10 times of normal dosage should be expected.

- Package and Storage:

25kg inner liner polyethylene (PE) bag, outer plastic woven bag,, or confirmed by clients. Storage in room shady and dry place.

Keywords: TTA China,Methylbenzotriazole(TTA)

- Corrosion Inhibitor for Hydrochloric Acid Cleaning

- Properties and Usage:

This product is a kind of imidazoline corrosion inhibitor. When cleaning metal using hydrochloric acid, this product can effectively inhibit steel corrosion.

- Specification:

| items | index |
| --- | --- |
| Appearance | Dark brown liquid |
| Solid content，% | 50.0 min |

- Usage:

The condition for using this product is that the cleaning media is hydrochloric acid and the cleaning object is black metals. It is suitable for acid cleaning of all types of high, medium and low pressure boiler, large scale of equipment and pipelines. When the dosage is 1-3‰, The corrosion ratio will be lower than 1g/m2•h.

- Package and Storage:

25kg or 250kg in plastic barrel, or confirmed by clients. Storage for ten months in room shady and dry place.

Keywords: Corrosion Inhibitor

- XT-0100 Antiscalant and Dispersant for RO Membrane

- Properties:

XT-0100 is a high-effective scale inhibitor, it is suitable for reverse osmose (RO), nanofiltration (NF) and ultrafiltration (UF) system. It can inhibit the scale deposit on membrane surface, improve water quality, lower operation expanse. This product has the following properties:

(1). Inhibit inorganic scale formation for a wide concentration span, the largest permitted LSI value is 2.8 when no acid is added.

(2). Not flocculate with ferric oxide, aluminia oxide or silica oxide to form suspended substance;

(3). Inhibit the pollution from ferric, aluminium or heavy metals pollutants. The permitted ferric concentration for inlet water supply can reach to 8.0ppm.

(4). Inhibit the flocculate and deposit of silica, the permitted silica concentration for condense side can reach to 290ppm.

(5). Be used in CA, TFC, NF and UF membranes for RO system.

(6). Good solubility and stability.

(7). Effective in pH 5-10.

- Specification:

| itemss | index |  |
| --- | --- | --- |
| Appearance | Clear liquid | Clear transparent liquid |
| pH Value，（1% water solution） | 2.0±0.5 | 2.5±0.5 |
| Density （20℃）g/cm3 | 1.08±0.05 | 1.45±0.05 |
| Main content | Micromolecular containing P | Micromolecular containing P |
| Decomposition product under high temperature | orthophosphate | orthophosphate |

- Package and Storage:

The original package is 8 times condense liquid, 5 gallon (27.55kg) per barrel. After diluting 8 times, 220.4kg per barrel.

- Usage Method:

The dosage is determined by water quality analysis and condition of reverse osmose system. In the recommended range of dosage, most scales can be under control such as calcium carbonate, calcium sulfate, barium sulfate, ferric hydroxide, aluminium hydroxide and silica.

The following formula can be used to calculate the XT-0100 volumes required to add to medicine box:

where: U—— condense liquid volumes required, Litre, (L)

Q—— reverse osmose water supply flow, tons/hour (T/h)

a—— dosage required, gram/ton, (ppm, g/T) (standard liquid)

V—— effective volume of medicine box, litre (L)

ρ—— density of the XT-0100, kg/L, the density is 1.45

x—— the actual flow of medicine operation pump, litre/hour (L/h)

1000 —— conversion coefficient

8 —— condense index

Notes: the value a (dosage required) can refer to the special software of QingLi Company.

Keywords: Antiscale and Dispersant,Antiscale and Dispersant for Reverse Osmose Membrane

- XT-191 Antiscalant and Dispersant for RO Membrane

- Properties:

XT-191 is mainly used in RO membrane system, it can be used as antiscalant and anti-choking agent in high salt water and drinking water. It has the following properties:

1.  Used in many water quality system, high scale inhibition ability.

2.  Lower scale deposit and reduce RO pipeline cleaning frequency.

3.  Reduce or replace the acid fill treatment.

4.  Good economic effect.

5.  Suitable for all RO pipeline type, and as an effective ferrium insulator.

6.  Stable and effective than calgon(SHMP).

7.  High water flux density for RO pipeline.

- Specification:

| items | index |
| --- | --- |
| Appearance | Light yellow transparent liquid |
| pH Value，（1% water solution） | 10.0-11.0 |
| Density （20℃）g/cm3 | 1.16-1.36 |
| Solubility | Mix well in any ratio |

- Package and Storage:

25kg barrel or confirmed by clients. It can be stored for one years.

- Usage Method:

For best effective, XT-191 should be added before static mixer or cylindric filter, the dosage of 1-4mg/L is expected, it can be diluted by RO liquid or by deionized water.

Notes: extra or insufficient dosage will do harm to the RO membrane.

Keywords: Antiscale and Dispersant,Antiscale and Dispersant for Reverse Osmose Membrane